Good afternoon,

We are providing an update regarding our site visit yesterday to Units F-304 and F-204 and the ongoing investigation of the slab edge and post-tensioned cable conditions.

The contractor reported deteriorated concrete, elevated moisture within the concrete surrounding the exposed cable embed areas, rotting of the header below that appears to be due to water intrusion from the removed sliding glass door fasteners.

As part of our initial assessment, we performed Swiss hammer testing at various locations along the slab edge to estimate the compressive strength of concrete. The testing at the areas evaluated near the slab edge indicated estimated compressive strengths exceeding 5,000 psi, which is considered sufficient for the existing slab. This testing is intended to provide a preliminary indication of the concrete condition. We also performed moisture content readings of the concrete. The readings obtained were on average 1% relative moisture content, below the 3.5% acceptable moisture content limit.

Next Steps

To further evaluate the extent of the deterioration and determine the appropriate repair scope, we recommend the following:

- Remove the sliding glass door at Unit F-204 to provide access for further investigation.

- Remove the deteriorated header at Unit F-204

- Perform a comprehensive assessment of the slab edge concrete and post-tensioned cable conditions

- Based on the exposed conditions, determine the extent of concrete repairs and any required repairs to the post-tensioned cable system.

We will provide additional updates as the investigation progresses and further conditions are exposed.

Please let us know if you have any questions.

Best,

|  | DYANI COLON EECON ENGINEERING SERVICES STAFF ENGINEER. P: (239) 512-4450 ext 205. C: (786) 333-2340. E: dyani.colon@eecon-eng.com. 5688 Strand Ct.. Naples, Florida 34110. |
| --- | --- |